EXPERIENCE OF USING LASER DRILLED S.S. SCREENS AT CHAUDHRY SUGAR MILLS

M MAQSOOD  ALAM

Project Director Choudri Sugar Mills Gojra

M TAHIR JAVED  HASHMI

Dy.General Manager Gojra Samundri Sugar Mills

INTRODUCTION

Due to high percentage of molasses in Pakistan, the purity of final molasses is one of the most important parameters in controlling the losses of sugar during processing.

It is well known that the purity of final molasses is the net results of the Cane quality, Staling in the field/cane yard, sanitation at the mills, juice clarification, the boiling scheme, performance at pan station and the performance at  the centrifugal station etc .

In this paper, we will concentrate on the practices at the centrifugal station, more precisely the effect of using different type of screens.

Normally Chrome coated Nickel screen of 0.06mm aperture are used at CFW centrifugals. Some Sugar Mills are also using Chrome coated Nickel screens of 0.04mm aperture, with an aim to reduce the final molasses purity. These screens deform very quickly so that at least two screens per centrifugal per season have to be used.

To solve this problem Stainless Screens have been developed in Australia which are being used in many countries of the world.

In this paper performance of a LASER DRILLED CHROME COATED S.S. screen has been compared with a 0.04mm Chrome coated Nickel screen.

WHAT IS A LASER DRILLED S.S. SCREENS

It is a stainless steel screen on which the Chrome layer is electroplated. Stainless steel being a hard material, it is drilled with a laser beam. As a result the shape of the slot is oval, as compared to Nickel Screen in which case it is rectangular.

This means that when we say that it is a 0.06mm SS screen, this size is only in the middle of the slot, other parts of the slot will be smaller in size. In case of a Nickel Screen the slot size will be uniform.

MATERIAL & METHODS

A laser drilled Chrome plated SS screen of slot size 0.06X2.67mm, with an open area of 6.5% was installed in one of the CFW centrifugal at our sugar mills. At the same time another CFW machine was fitted with a Chrome plated Nickel screen of slot size 0.04x2.68mm with an open Area of 9 %.

Same C-Massecuite was purged on both centrifugals. All parameters like RPM, motor power, No. of belts, curing temperature of C-Massecuite and electrical load (Amps) were kept vigilantly matched of both the machines.

Comparison of results of Laser drilled S.S. screen with Nickel/Chrome screen was made till the end of the season.

The samples of C-massecuites, C- Sugars and final molasses were collected regularly, on 2 hourly basis, from both the machines separately.   Their composite samples were made for 24 hours.   Analysis of these composite samples was performed in laboratory on daily basis.

Weekly averages of these results have been used for comparison of the above screens.

RESULTS AND DISCUSSION

Results of the above trial are being given as table 1.

(Table 1)

CHAUDHRY SUGAR MILLS LIMITED GOJRA

PERFORMANCE COMPARISON OF LASER DRILLED S.S. SCREEN

VS

CHROME NICKLE SCREEN

| Sr.# | Description | Laser Drilled | Hard Chrome Nickle | Remarks |
| --- | --- | --- | --- | --- |
|  |  | Screen | HCRDS Screen |  |
| 1 | Type of Centrifugal Used | K-1100 | K-1100 | Same |
| 2 | RPM of Centrifugal | 2100 - 2150 | 2100 - 2150 | Same |
| 3 | Screen Open Area % | 6.5 | 9.7 |  |
| 4 | Slot size mm | 0.059 | 0.04 | Slot size of laser screen is larger |
| 5 | Average Massecuite | 7.5 | 8.1 |  |
|  | Flow Rate T/Hour |  |  | Higher in the Ni Screen by about 8%. |
| 6 | Curing Temperature Co | 49-50 Co | 49-50 Co | Same |
| 7 | Average Molasses flow rate T / Hr. | 4.2 | 4.5 | Higher in the Ni Screen by about 7%. |
| 8 | Average Massecuit Purity purged | 52.88 o | 52.88 o | Same |
| 9 | Average C- Sugar Purity obtained | 80.09 | 79.59 | Higher in the Lasser screen by about 0.5o. |
| 10 | Average Final Molasses Purity | 34.38 | 35.01 | Lower from Lasser Drill Screen by about 0.63o. |
| 11 | Electric load on Centrifugal | 92-95 Ao | 92-95 Ao |  |

From these results it can be observed that

- Massecuite and molasses flow rates through normal chrome plated nickel screens are higher by about 7/8 % as compared to laser drilled S.S. screens.

However it may be noted that Chrome Nickel screen used in this trial has about 50% higher open area (9%) as compared to laser screen (6.5%).

- The purity of C- sugar purged from laser drilled screen is higher by about 0.5° as compared to the nickel screen.

- The purity of final molasses purged through laser drilled S.S. screen is lower by about 0.63° as compared to 0.04 mm chrome plated nickel screen.

FINAL MOLASSES PURITIES COMPARISON

In the above paragraph only average purities of the Final Molasses have been mentioned. Weekly comparison of Final molasses purities is given as Table 2.

(Table  2)

FINAL MOLASSES PURITIES

| weeks | 1st | 2nd | 3rd | 4th | 5th | 6th | 7th |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Date | 23/1 to 29/1 | 30/1 to 5/2 | 6/2 to 12/2 | 20/2 to 26/2 | 27/2 to 5/3 | 6/3 to 12/3 | 13/3 to 19/3 |
| Laser Screen | 32.96 | 32.92 | 32.6 | 34.74 | 35.49 | 35.64 | 36.33 |
| Nickle screen | 33.38 | 33.65 | 33.37 | 35.7 | 35.76 | 36.28 | 37.22 |
| Difference | 0.42 | 0.73 | 0.77 | 0.96 | 0.27 | 0.64 | 0.89 |

Note:-

1.	Laser drill screen was fitted on 18-12-11 and is still intact.

2.	Nickle screen was fitted on date 05-12-10. It was replaced with new screen

on 26-02-11 due deformation and erosion of nickle polish.

The same figures are being illustrated in the graphical form as fig 1.

(Fig. 1)

CHOUDHRY SUGAR MILLS

COMPARASION OF FINAL MOLASSES PURITIES LASER SCREEN VS Ni SCREEN

From these figures it can be noted that the final molasses purity of the laser drilled screen remained lower in comparison to nickel screen throughout the season.    In the 1st week, the purity difference of both types of screens was about 0.420, but it increased to 0.730 in the 2nd week. It increased further to about 0.77⁰ in the 3rd week.   At this stage Chrome plated screen was dismantled and examined.   It coatings were found de-polished and deformation in the shape of the slots was observed.

In the 4th week, the purity difference further increased to 0.960. Then it had to be decided to replace the nickel chrome screen.  Where as laser drilled remained intact through out this period of observation.   After replacing chrome nickel screen the increase in the difference of purities of two screens with time was repeated again.

This trend of increasing the difference in final molasses purities with time is illustrated

as fig 2.

(Fig. 2)

TREND OF FINAL MOLASSES PURITY DIFFERENCE WITH TIME

COST BENEFIT ANALYSIS.

Cost benefit analysis of using laser screen shows cost benefit ratio of about 1:8.Calculations are given as annex 1.

CONCLUSION.

- Laser drilled chrome plated S.S. screen has lower final molasses purity as compared to the Chrome plated nickel screen.

- C-sugar purged on laser screen has comparatively high purity.

- Losses of sugar in final molasses purged through chrome plated nickel screen increases with time due to removal of chrome layer from nickel screen.

- Break down time of laser drill screen fitted machine is less due to no periodic replacement of the screen.   Once a set of screen is fitted.   It remains intact through out the season.

- Laser drilled chrome plated S.S. screen is cost effect due to its longer life. The manufacturer claims 3 seasons under Pakistan conditions.

In our case the screen has been used for one season, there is no sign of deformation. The condition of the screen suggests that it can be used for at least one more season if not two.

- On the basis of Lower final Molasses purity and longer life, The cost benefit analysis shows a cost to benefit ratio of 1:8

COST & BENEFITS ANALYSIS OF USING LASER SCREENS

FOR A TYPICAL 8OOO TCD MILL

TECHNICAL RESULTS

Comparison of final molasses purity by using Laser Drilled Stainless Steel Screen Vs Nickle Screens

Figures at Chaudhary show an average difference of 0.63⁰.We are taking a difference   of 0.5⁰

S. No.	        Description

1	Difference in F.M.Purity								0.5

FINANCIAL CALCULATIONS

2	Crushing							Mds	       17,500,000.00

Tons	             700,000.00

3	Type of Machine								       K 1100

4.	No. of C-Fore Worker of machines							   6

5.	Laser screen sets required ( 1/2 set for each

Centrifugal because laser screens last for 2 seasons )		Sets			   3

6.	Price of one set K1100 Screen				US $	 6490.00	    6,490.00

in RS							Rs	669768.00	669,768.00

7.	Total cost of Laser Screens			Rs	20,09,304.00          2,009,304.00

8.	Nikle Screen set required

( 2 set per centrifugals / Seasons )	          Sets  		 12

9.	Cost of Nikle Screen /set		 		Rs	 	 38,000.00

10.	Total Cost of Nikle Screens			Rs	            456,000.00

11.	Difference in costs of screens			Rs	         1,553,304.00

12.	Gain in recovery due to difference in Molasses purity  %	     0.036%

13.	Net increase in production due to gain in recovery  M.Ton 252.00

14.	Price of Sugar 					Rs/Tons             65,000.00

15.	Price of Sugar minus Sales Tax	.		Rs/Tons	 60,185.19

16.	Increase in revenue due to extra sugar	Rs	      15,166,666.67

17.	Difference in cost of screens			Rs 	        1,553,304.00

18.	Net gain by using Laser Screen			Rs	     1,51,66,666.00

19.	Cost Benefit Ratio                       (17) : (18)

NOTE: -

**Import duty etc, except Sales Tax.

# Text boxes

Annex 1